## Slide 1
Yutaka Yamada (SIT, IEA-HTS OA)
HTS Activity in China
1
Jan. 30, 2016 at RSE, Milan, Italy
IEA-HTS-Exco, Milan
Notes: Today I would like to introduce “HTS Road Map for Power Applications”, which was done by IEA-HTS-IA.
Here are the authors, me, xxx, yyy, and the committee members of IEA-HTS-IA.

## Slide 2
HTS
EU
China
Korea

## Slide 3
Electric Power Consumption for the past decade
China
US
Japan
Increase in China doubles that in Japan.
“Key World Energy Statistics 2016” in IEA - Free publications
India
Russia
Brazil
Electric Power Consumption (100milion kWh)

## Slide 4
R&D Programs for Superconductivity in China
Main goals:
Manufacture technology of Superconducting materials for practical applications.
Superconducting technology: cable, FCL, magnet, and filter.
Main Projects including:
-- Manufacture techniques of high-performance Coated Conductor superconducting tapes
-- Manufacture techniques of superconducting strands for high-performance MRI application
-- Nb3Sn superconducting wires for high-field application
-- large capbility HTS Superconducting cables
-- High voltage level superconducting FCL
Principal Investigator: Prof. Pingxiang Zhang
Total fund: 200 Million RMB (FY2011-FY2015) to 32 groups with more than 300 researchers.
1.National High Technology Research and Development Program (863 Program)
～15MUS$
～100MUS$ including other 4 programs
Notes: For those who may not know alstom let me give you few intoductory words on our company

## Slide 5
China HTS Activity
Prf. Cai of Shanghai Univ.

## Slide 6
China
Dr. Xiao of CAS, Beijing

## Slide 7
Visit to Shanghai and Xian
1.2億人
14億人
2.6億人
1億人
1億人
0.7億人
0.3億人
0.5億人

## Slide 8
Visit China: Shanghai, Xian
SSTC in Shanghai.
SCSTC in Shanghai.
SSTC in Shanghai.

## Slide 9
NIN and West Superconductor:Nb3Sn, Bi2212, 2223, MgB2…..
Prof. Zhang of NIN, Xian

## Slide 10
Fabrication of large size NbTi/Cu composite billet
WST developed the fabrication technology to make large size NbTi/Cu billet with high quality long wires
Subelements
NbTi
Nb
Cu stablizer
Single filament
Cu
Cu
450kg billlet with 2616 filaments in one step assembly process. Fill ration reaches 98%.

## Slide 12
CC of China
Prf. Cai of Shanghai Univ.

## Slide 13
Development of km-level YBCO CC by MOCVD/PLD
4. MOCVD-YBCO layer deposition technology
Capability > 1000m Width of tape 12mm
Speed：50 -100 m/h Thickness of YBCO 1-3 μm
The MOCVD system can deposit 1-3μm YBCO layer with sharp texture on km-level IBAD-MgO layer.
Ic=280 A/cm-width @77K

## Slide 14
5. PLD-YBCO layer deposition technology
The PLD system can deposit 1-3μm YBCO layer with sharp texture on 500m-level IBAD-MgO layer.
Ic=500 A/cm-width @77K
SSTC, Shanghai Jiao ton Univ.

## Slide 15
SCSTC, Shanghai Univ.
Prf. Cai of Shanghai Univ.

## Slide 16
Sharp cube textured (~100%) Ni5W tapes with the level of hundred meters were obtained by conventional metallurgy method.
Content of cube texture in Ni7W and Ni9W tapes reaches 99.5% and 94% respectively.
Thickness~66 μm
Width=10 mm
Length>500 m
NiW-alloy ingot
Long-length & Textured Ni5W，Ni7W and Ni9W tapes for CC
at NIN, West Superconductor

## Slide 17
Dr. Xiao of CAS, Beijing
Cable, FCL and MRI are active.

## Slide 18
With the sophisticated hot rolling line, cold rolling line and foil processing line as well as inspection facilities, most of its equipment are advanced nationally and some of even worldwide. It’s designed out put is 200,000 tons per year.

## Slide 20
FCL from low to high voltage

## Slide 24
Progress of SC and its application in China (2011-2015)
The R&D of superconducting materials and applications in China cover all the fields today.
2011
2015
2012
2013
2014
LTS：
Starting mass production
180t NbTi and 30t Nb3Sn strands for ITER, 100t strands for MRI and HEP application
YBCO CC: 50m, Ic=140A@77K
Laboratory scale
Cable：
380m, 10000A DC
YBCO CC: 1000m, Ic=280A@77K
Industry scale
FCL：
220kV, 3 Phase
FCL：
550kV, 3 Phase
Power DEMO：HTS Power Substation
Materials
Application
Prf. Zhang of NIN, Xian.

## Slide 25
Summary
/ Up to now, 100MUS$ invested for 2011 to 2015
/ Wire produced from LTS to HST (Bi2223, 2212, YBCO, MgB2)
in the areas of Shanghai for YBCO
Xian for LTS, Bi, MgB2
/ Active Application
Cable, FCL
MRI for the market in the near future
/ Further investment will be expected also after 2016.