## Slide 1: Japanese HTS PJ now and future
Energy Conservation Technology Department
Susumu Kinoshita
IEA High-Temperature Superconductivity (HTS) Workshop
"HTS Applications in the Power Sector”
30th Jan 201７
Milano
Notes: .

## Slide 2: Outline
2
1. Introduction
  - What’s NEDO ?
  NEDO’s R&D Projects on Superconductivity
2. NEDO HTS Project
- June 2016 – March 2021

## Slide 3
As Japan's largest public management organization promoting research and development as well as the dissemination of energy, environmental and industrial technologies, NEDO has a crucial mission to carry out.
  Addressing energy and global environmental problems
  Enhancement of Japan’s industrial competitiveness
Chairman: Mr. Kazuo Furukawa
Organization: -Incorporated administrative agency under the
Ministry of Economy, Trade and Industry (METI),
government of Japan
- Established in 1980
Location: Kawasaki City, Japan
Personnel About 920
Budget Approximately 129.8 Billion yen (2016 fiscal year)
(1.1 Billion US dollars)
What’s NEDO ?

## Slide 4
Bio/medical
Water
treatment
Energy storage
Renewable energy
Energy conservation
Electronics /ICT
Smart community
Environment/ clean coal
Robotics
Basic Research
Demonstration
Technology Development
Materials/nanotech
NEDO’s Technology Area

## Slide 5
NEDO’s R&D Project on Superconductivity
Materials,
Science &
Processings
Power Device
Applications
Fundamental Materials Science
& Engineering
Superconducting
Generator((SCG )
Superconductive Generator Equipment(LTS)
and Materials (Super-GM)
Generator
SMES system (LTS)
Basic Technology
SMES system
(LTS)
SC Power
Network
(LTS-SMES)
Flywheel
HTS Flywheel
Energy Storage
SC Magnetic
Bearing for FW
SC Power
Network
System (FW)
AC Power Device
Cable, FCL, etc.
AC Power
SC Equipment
(Super-ACE )
Bi-Cable( AC)
( Field Test )
SMES
Fundamental Technologies for
Superconductivity Applications Phase I, II
YBCO C.C. etc
Reduction of Rare Earth Usage for Motors
High Jc
BSCCO
Wire
MAGLEV
M-PACC
SMES, Cable( AC),
Transformer, & C.C.

## Slide 6: Outline
6
1. Introduction
  - What’s NEDO ?
  NEDO’s R&D Projects on Superconductivity
2. NEDO HTS Project
- June 2016 – February 2021

## Slide 7
NEW NEDO HTS Project
“Project to Promote Commercialization of
High-Temperature Superconductivity
Technology”
Period: June 2016-Februrary 2021 5years
Budget:€68M (120yen/€ 5years)
€12.5M (2016FY)

## Slide 8: Development Items and Targets
Cate gory | Items | Subsidy From NEDO | Target | Contractor
HTS Power Transmission Development | ①Commercialization Development of HTS Power transmission cable system （2016～2018） | 50% | ・Establishment of safety and evaluation standards for HTS cable system ・Establishment of high efficient cooling system ＣＯＰ：>0.11, Inspection period：40,000h ・DC power transmission : Establishment of design/operating guideline | Tokyo Power Electric HD, Sumitomo Electric Industries, Furukawa Electric Industries, Mayekawa MFG I-SPOT
 | ②Basic technology Development for applying transportation （2016～2020） | 100% | ・Establishment 2km long cooling system and demonstration cooler size : ２ｍ３ /kW, Pump：0.6MPa, Flow rate 50L/m ・Establishment of design/evaluation/maintenance standard | Railway Technical Research Institute
High Magnetic Field Magnet System Development | ③Technology Development of High stable Magnetic Field HTS Magnet system （2016～2020） | 100% | ・Imaging Demonstration of ３Ｔ Half size Magnet Coil system Magnetic Field uniformity <100ppm Magnetic Field stability <1ppm/ｈ ・Establishment design standard for ３T MRI coil shape, cooling ability, cryostat etc. ・Technology Development of superconducting contact （<10-12Ω） | Mitsubishi Electric Advanced Industrial Science and Technology Furukawa Electric Industries
 | ④Commercialization Development of HTS wire for High Magnetic Field Coil （2016～2018） | 100% | ・Improvement of High Magnetic Field REBCO wire： Ave current density >400A/mm2 @30K, ７Ｔ ・Ｉｃ deviation （（Ic ave.-Ic min.）/Ic ave.）< 0.15 for 1km long wire | Fujikura Advanced Industrial Science and Technology
 |  | 50% | ・REBCO wire production rate > 50m/h | Fujikura

## Slide 9
HTS Power Transmission Development
High Magnetic Field Magnet
System Development
①Commercialization Development of HTS Power transmission cable system
（2016～2018）
②Basic technology
Development for
applying
transportation
（2016～2020）
③Technology
Development of High
stable Magnetic
Field HTS Magnet
system
（2016～2020）
④Commercialization
Development of HTS
wire for High
Magnetic Field Coil
（2016～2018）
2017FY
2018FY
2019FY
2020FY
2016FY
●６６ｋＶ，66kV, 275kV Establishment of safety
and evaluation standards for HTS cable system
●In-grid Operation, dismantling and research
●DC power transmission
: Establishment of design/
operating guideline
●Small size cooling system
●LN2 Pump
●Insulating Pipe （Cable）
●Laying long HTS
Feeder
●Estimation
●System maintenance study
●Development of ３Ｔ Half size Magnet Coil system
●Establishment design standard for ３T MRI
coil shape, cooling ability, cryostat etc.
●Development 5Ｔ Half size Magnet coil system
●Imaging by 5T Half size MRI
●Improvement of High Magnetic Field REBCO wire
●Improvement stability in long length
●Improvement Throughput
Promotion to Commercialization
Putting Wire
to Practical use
●Technology Development of superconducting contact (<10-12Ω)
●Trial coil production by superconducting contact
/Evaluation
●Design spec.
for cable
●Estimation standard
for Safety/ reliability
Contents and Period

## Slide 10
Trans
154/66 kV
200 MVA
Site
office
Monitoring
house
CH
CB2
CB1
LS1
LS2
LS3
CB
Joint
Cooling
system
house
AC Transmission cable system
Notes: This slide shows the cable system after construction.
Cable with straight, cable with 180 degree bent,
Cable-to-cable joint, terminations, and cooling system.

## Slide 11
Refrigerator
Pump
Unit
Flow meter
Sub-cooler
(buck-up of
refrigerator)
Reservoir
● Capacity is 5 kW
● COP 0.1
● Maintenance
interval is > 30,000 hours
Brayton refrigerator cooling system
AC Transmission cable system
Notes: 11

## Slide 12
●Purpose
To promote Commercialization of large capacity, low loss, long distance DC transmission cable system,
1)Verifying various characteristics using 1 km superconducting cable
system
2)Summarizing Guidelines on design, construction, operating, maintenance,
etc.
●Period：24 Jun 2016～28 Feb 2017 (8 months)
●Budget：200M yen （Subsidy 50%)
●Member：I-SPOT
（Chiyoda corp.,
Sumitomo Electrical Ind.,
Chubu Univ.,
Sakura Internet Inc.）
●Features
①Low heat intrusion
Straight tube : >1W/m
②Heat shrinkage
Helical deformation
③Multi-joints (two joints)
DC Transmission cable system
R & D Items | 1Q | 2Q | 3Q | 4Q
Item I |  |  |  | 
[1] Evaluation of liquid nitrogen circulation cooling performance simulating long distance |  |  |  | 
[2] Evaluation of conduction characteristics of superconducting cable system |  |  |  | 
[3] Evaluation by severe condition test |  |  |  | 
[4] Evaluation of long-term operation performance |  |  |  | 
[5] Residual performance confirmation test |  |  |  | 
Item II |  |  |  | 
Create design, operation and maintenance guidelines |  |  |  | 

## Slide 13
CSJ
NJ
Nominal Current | ２５００A
Capacity | ５０MVA
Length | １０００ｍ
Heat Intrusion
>1W/m
DC Transmission cable system
Section 2 : 125m
Section 3 : 372.5m
Section 1 : 468.8m
Cable Joint
Cable Joint
Terminal B Terminal A
Cooler, Pump
Former Conductor Conductor Shield
Cushion
Insulation
Protection
Return pipe SUS50A
Carbon steel pipe 300A
Shield Al
Support FRP
Cable pipe SUS65A
Cable
Multi-Insulation
Insulation
Multi-Insulation

## Slide 14
1km System
Pipe
Cooler system
Turbo Brayton 2kWx2+Starling 1kWx2
Terminal
Cable
Cable joint
DC Transmission cable system

## Slide 15
Background・Problem
・Promotion of development of fundamental superconducting technology
・Superconducting technology is expected to be applied to power transmission cables.
Especially social infrastructure such as railroad.
Issues in the railway site
Social Needs
・The power loss due to the resistance of conventional cables is large. ・There is no site to establish a substation when there is a demand for
enhancement of transport capacity, there is no countermeasure.
Effects
・To reduce the regeneration expiration and transmission loss. ・Voltage compensation effect.
・Consolidation of substations.
・Load leveling of substation and suppression of rail galvanic corrosion.
Realization of a compact long-distance cooling system that can be used at railway sites
DC Feeder cable system (Railway)

## Slide 16
Items |  | 2016 |  | 2030
①Establishment km-class long cooling system |  |  |  | 
(１) | Compact size cooling system （RTRI, Meyekawa） | Installation volume 10 m3/kW | Installation volume 2 m3/kW | 
(２) | LN2 pump system （RTRI, IHI） | Head：0.3 MPa Flow rate：25 L/min | Head：0.6 MPa Flow rate：50 L/min | 
(３) | Insulation pipe technology development (RTRI, MESCO) | Heat intrusion： >4 W/m Regular evacuation | Heat intrusion ：2 W/m Once 1 year evacuation | 
②Establishment of design/evaluation/maintenance standard |  |  |  | 
(１) | Evaluation Technology （RTRI, Tokyo Univ.） | ― | Electric field analysis of current lead under nitrogen gas environment | 
(２) | Maintenance technology （RTRI, Kyushu Univ., Mie Univ.） | ― | Establishment of application guidelines for system maintenance technology | 
DC Feeder cable system (Railway)
target

## Slide 17
Main Objective
○Test producing 3T and 5T half size HTS coils for MRI
○Measurement of field uniformity and stability
○High current density coil (>200A/mm2 at 7T)
○Design of 3T whole body MRI magnet by HTS
The work will be held 2016-2020
Development of a high temperature superconducting magnet system having high stable magnetic field
３T
５T
1st:2016~2018
2nd:2018~2020
Imaging to demonstrate high stable magnetic field and high homogeneous magnetic field
MRI magnet system

## Slide 18
Test half size 3T HTS coil for MRI
A design of a half size HTS 3T-coil
Active shield coil
Main coil
φ580mm
φ1200mm
L:980mm
Specification of the half size 3T HTS Coil
Inner diameter | 580mm
Maximum outer diameter | 1200mm
Axial length | 980mm
Operating central field | 2.9T
Maximum field | Bzmax=4.2T,Brmax=2.9T
Current density of coil | 121A/mm2
Inductance | 145H
Stored energy at operation | 1.6MJ
Field uniformity on design | 1.7ppm/250mmDSV
Leak magnetic field area | 2.5mX3.4m (0.5mT)
Cryostat will be designed next year.
Room bore is from 480mm to 500mmDia.
Imaging is a region of 150 mm or more in sphere
MRI magnet system

## Slide 19
SUMMARY
○ As a next-generation MRI, we started the research and development of high stable magnetic field coil system fundamental technology using the ReBCO superconducting coil.
○ We promote the development aimed at imaging verification magnetic field of 3 T of stability less than 1ppm / hr and uniformity of 10ppm / 20mmDSV.
○ As a result, we successfully verified measures for issues in these particular subjects. World's first MRI Images of Mouse fetus using a HTS 3T Test Magnet at 2.9T were obtained.
○Advance research and development to solve problems related to the manufacture of large-diameter magnets and obtain highly stable magnetic fields as a next-step project for practical application of the high temperature superconducting coils.
MRI magnet system

## Slide 20: Development of HTS magnet systems with a high uniformity magnetic field
Completion of persistent mode technologies for a ３Ｔ HTS-MRI magnet
Achievement; HTS joint with the resistivity less than 10-12Ω
PCS
HTS joint
HTS solenoid coil
[Design: tentative]
1 Tesla
ID 120mm
OD 200mm
Length 200mm
Target (2018)
Construction of a 1-Tesla REBCO solenoid coil with the HTS joints
Ic measurement
HTS DP coil
PCS
Heater
DC current
77 K
Joint-R measurement
20 K
2.5 x 10-12Ω
Time [sec]
Centerfield of DP coil [T]
REBCO tape joint

## Slide 21
3-4nm dia.
~20nm
distance
corresponding
matching field
:5-7T
Plan view
Cross sectional view
100 nm
Chart: B=5T
| 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
4.2K | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
20K | 1272.7528 | 1235.7389 | 1226.0173 | 1223.6791 | 1234.8458 | 1257.8906 | 1289.9954 | 1330.5327 | 1362.2684 | 1378.7182 | 1371.1967 | 1362.2212 | 1334.1467 | 1290.8439 | 1270.9171 | 1233.2454 | 1202.4964 | 1176.5168 | 1176.0895 | 1164.9979 | 1167.4233 | 1190.3594 | 1230.0251 | 1241.2908 | 1281.4595 | 1309.9586 | 1343.0681 | 1453.4321 | 1626.6878 | 1719.9911 | 1836.0617 | 1879.4163 | 1936.827 | 2031.7617 | 2144.4076 | 2254.1957 | 2381.1027 | 2442.5727 | 2425.2731 | 2383.0972 | 2231.9721 | 2148.5053 | 2010.0328 | 1836.2089 | 1745.8867 | 1545.81 | 1477.7264 | 1414.8053 | 1353.7781 | 1322.8768
30K | 629.0437 | 643.4191 | 667.5758 | 696.8445 | 739.5363 | 785.401 | 826.0717 | 884.6649 | 922.8174 | 944.5424 | 948.1178 | 929.7491 | 899.7845 | 858.136 | 820.8315 | 781.9866 | 743.964 | 713.175 | 684.549 | 660.4068 | 639.5035 | 623.5197 | 611.4036 | 604.6233 | 603.8714 | 605.7919 | 604.5241 | 611.574 | 652.969 | 690.9135 | 755.1516 | 794.9066 | 855.9872 | 932.1664 | 1054.6821 | 1232.9543 | 1407.4461 | 1465.7775 | 1362.8052 | 1218.2079 | 1043.0004 | 964.904 | 870.3778 | 824.8683 | 765.83 | 726.0296 | 720.7311 | 637.505 | 628.8817 | 626.9856 | 629.3973 | 642.8469
40K | 365.1198 | 387.3276 | 416.3716 | 447.9304 | 482.1776 | 523.7016 | 562.0496 | 611.3052 | 643.0146 | 664.1541 | 667.2064 | 649.6948 | 622.7514 | 588.6236 | 551.0509 | 523.5892 | 492.6945 | 466.9102 | 440.4228 | 418.8339 | 399.261 | 379.5751 | 362.2789 | 346.3571 | 331.6812 | 321.9806 | 314.3478 | 294.3306 | 272.9083 | 272.0885 | 281.6195 | 294.4655 | 317.2925 | 354.5602 | 420.921 | 521.5718 | 662.2253 | 695.0992 | 585.8892 | 467.8022 | 390.1836 | 341.0895 | 315.2403 | 288.8283 | 281.649 | 294.8054 | 316.4939 | 335.9069 | 355.4833 | 373.9907
50K | 231.2531 | 248.9914 | 268.152 | 288.3352 | 312.529 | 338.9077 | 365.5933 | 399.6728 | 421.891 | 438.2373 | 441.806 | 428.9775 | 409.5794 | 383.4848 | 357.9374 | 336.2288 | 315.2118 | 294.9017 | 282.0176 | 266.6752 | 254.3354 | 240.9945 | 230.6516 | 220.0132 | 209.4249 | 202.3068 | 196.7417 | 190.2635 | 182.9874 | 174.5637 | 170.0719 | 165.5442 | 160.6192 | 156.68 | 152.4847 | 149.6529 | 145.7089 | 144.0924 | 144.4929 | 147.1916 | 155.9989 | 178.9755 | 223.0979 | 288.2298 | 282.2086 | 231.0975 | 166.8327 | 152.1716 | 151.8111 | 155.824 | 176.7484 | 196.176 | 211.4637 | 225.2604 | 237.9108
65K | 92.4753 | 97.7421 | 103.4177 | 110.3501 | 119.148 | 128.6893 | 139.4278 | 152.4495 | 162.1002 | 168.4787 | 168.4057 | 162.1531 | 152.9826 | 141.707 | 132.0224 | 123.2371 | 114.9816 | 107.7987 | 102.5364 | 97.668 | 93.5236 | 90.334 | 87.8386 | 85.6053 | 83.4845 | 81.865 | 80.4563 | 78.7116 | 76.6964 | 74.0526 | 72.5485 | 70.8619 | 69.2969 | 67.8443 | 66.4584 | 64.9253 | 63.8654 | 62.9986 | 62.5356 | 63.2776 | 66.5432 | 75.1053 | 95.3905 | 105.5673 | 91.7912 | 79.9123 | 68.2 | 65.3561 | 66.3181 | 68.6329 | 76.1116 | 81.9779 | 86.1108 | 89.4949 | 93.1835
B // c
B // ab
Ic(B//c) ≠ Min. Ic
at higher temp.
1.0mm
High performance by artificial pinning centers
and structural factor optimization
Improvement of HTS wire

## Slide 22
Cumulative failure
probability (1 mm3)
m=2.5
m=3.2
m=21
good agreement
Technology for improving uniformity of long wire performance
Reliability evaluation technology development
Peeling strength characteristics of long wire
～50MPa
～３MPa
Improvement of HTS wire

## Slide 23
Research and development of low loss structure wire for high magnetic field coil
Performance improvement of wire rod and simulation of electromagnetic response by thinning processing for low loss structure wire for high magnetic field coil
in collaboration with H. Zhang (Univ. Bath, UK)
Scribing tape wire
Current distribution of scribing tape wire
J/Jc
High performance thinning technique by scribing the superconducting tape wire
Considering the model (ρs ~ Jn - 1) of nonlinear resistance in superconducting thin wire and the normal conducting resistance (ρn) between fine wires, we simulate Maxwell equation numerically.
Filament Ic(A)
Filament Ic
To eliminate variations
Improvement of HTS wire

## Slide 24: Thank you for your attention.
Energy Conservation Technology Department
Notes: ご清聴ありがとうございました。